BEACON

B E H A V I O U R — A W A R E   B A T T E R Y   M O N I T O R I N G

Complete Project Report

From lithium-ion degradation to a validated monitoring system

What this report covers. It begins with how a lithium-ion cell works and why it degrades, explains what a battery management system must do and where state-of-health estimation becomes hard, then presents BEACON: what was built, what it found, what it now does on physical hardware, and what remains.

Department of Computer and Communication Engineering

18 September 2026

## Contents

# PART I

      Background: Cells, Degradation and Battery Management

This part establishes the frame of reference and the terminology the rest of the report uses. It is deliberately brief on material a reader with battery background already holds, and dwells only where a specific mechanism becomes load-bearing for a later result — in particular Section 2.3 on degradation modes and Section 4.2 on the temperature dependence of measured capacity, both of which are relied on in Part III.

## 1. The Lithium-Ion Cell

### 1.1 Operating principle

A lithium-ion cell stores energy by shuttling lithium ions between two intercalation hosts. On discharge, lithium de-intercalates from the negative electrode — typically graphite — travels through the electrolyte and separator, and intercalates into the positive electrode; the compensating electrons travel through the external circuit and do the useful work. Charging reverses the process. No material is consumed in the ideal case, which is what makes the chemistry rechargeable, and the near-absence of phase change in the host lattices is what gives it long cycle life relative to earlier chemistries.

The separator is an electronic insulator and an ionic conductor. Its failure — by puncture, by thermal shrinkage, or by penetration from a lithium dendrite — is the proximate cause of internal short circuit and thermal runaway, which is why protection is treated in this project as a hardware function that must not depend on software.

### 1.2 Chemistry and its consequences

The positive-electrode chemistry determines most of the trade-offs a system designer inherits:

| Chemistry | Designation | Character | Consequence for monitoring |
| --- | --- | --- | --- |
| LiCoO₂ | LCO / ICR | High specific energy, poor thermal stability, moderate cycle life | Narrow safe operating window; the cell used in this project’s rig |
| LiNiₓMnᵧCoᵣO₂ | NMC | Balanced energy and life; the automotive workhorse | Well-shaped OCV curve; the assumed target application |
| LiFePO₄ | LFP | Excellent thermal stability and cycle life, lower specific energy | Very flat OCV plateau makes SOC estimation by voltage unreliable |
| LiNiCoAlO₂ | NCA | High specific energy, used in some EV packs | Similar monitoring profile to NMC |

The LFP row is worth noting even though this project does not use LFP: it is the clearest illustration that a monitoring technique can be chemistry-dependent. A state-of-charge estimator that leans on open-circuit voltage works acceptably on NMC and poorly on LFP, because the quantity it reads is nearly flat across most of the usable range. The equivalent warning for this project is developed in Part III: a health estimator can be protocol-dependent in the same way.

## 2. Why Cells Degrade

Degradation is not one process. It is a set of competing mechanisms whose relative rates depend on temperature, current, state of charge and depth of discharge — which is precisely why usage behaviour is a plausible predictor of health, and why this project was attempted.

### 2.1 Principal mechanisms

- Solid-electrolyte interphase (SEI) growth. The electrolyte is thermodynamically unstable at the graphite potential and decomposes to form a passivating layer. The layer is necessary — without it decomposition would not stop — but it continues to thicken, consuming cyclable lithium and raising impedance. Growth is approximately parabolic in time and strongly accelerated by temperature.

- Lithium plating. At low temperature, high charge rate or high state of charge, lithium deposits metallically on the anode surface rather than intercalating. Some is recovered on the next discharge; some is not, and some forms dendrites that can penetrate the separator. This is the mechanism behind charge-rate and low-temperature charging limits.

- Loss of active material. Repeated lithiation and delithiation cycles the electrode particles through volume change, causing cracking, loss of electrical contact, binder degradation and delamination. Depth of discharge is the dominant usage driver.

- Transition-metal dissolution. Metal ions leave the positive electrode, migrate, and deposit on the negative electrode where they catalyse further SEI growth. Accelerated by high temperature and high voltage.

- Electrolyte oxidation and gas generation. At high potentials the electrolyte oxidises at the positive electrode, consuming electrolyte and generating gas, which in a pouch format produces measurable swelling.

### 2.2 Calendar and cycle ageing

Calendar ageing proceeds with time regardless of use, driven mainly by SEI growth, and depends on storage temperature and state of charge. Cycle ageing is driven by throughput and adds the mechanical and rate-dependent mechanisms above. A real duty cycle produces both simultaneously, and separating them requires an experimental design that holds one constant — which is what the cohort structure of the datasets used here provides.

### 2.3 Degradation modes: the diagnostic vocabulary

Mechanisms are many; their observable consequences collapse into three modes, and this taxonomy matters for interpreting Part III:

| Mode | Meaning | Observable signature |
| --- | --- | --- |
| LLI — loss of lithium inventory | Cyclable lithium consumed by side reactions, chiefly SEI | Capacity fade with electrode slippage; the usual dominant mode |
| LAM — loss of active material | Electrode material no longer electrochemically accessible | Capacity fade with change in curve shape |
| Resistance rise | Impedance growth from film formation and contact loss | Power fade; voltage sag under load; reduced usable capacity at a fixed cutoff |

Load-bearing for Part III. The third row is the one to carry forward. Resistance rise reduces measured capacity at a fixed cutoff voltage without any lithium having been lost — and impedance is strongly temperature dependent. A capacity measurement taken cold therefore understates the cell. Section 13 shows this effect at roughly 8 SOH points in the data used here, before any degradation has occurred.

### 2.4 The knee point

Capacity fade is typically near-linear for a long period and then accelerates, often sharply. The transition is called the knee. It matters commercially, because end-of-life is usually defined at 80% of rated capacity and the knee frequently sits near it, and it matters statistically, because a model fitted on pre-knee data extrapolates badly through it.

## 3. What a Battery Management System Does

A BMS is not primarily an estimator. Its first duty is protection, and estimation is layered on top of a system that must remain safe when the estimation is wrong.

| Function | Description |
| --- | --- |
| Protection | Over-voltage, under-voltage, over-current, over-temperature and short-circuit cutoff. Implemented in hardware, in series, independent of firmware. |
| Measurement | Per-cell voltage, pack current, multiple temperatures. The foundation everything else rests on. |
| State estimation | State of charge, state of health, remaining useful life, state of power. |
| Cell balancing | Passive (dissipative) or active (charge-shuttling) equalisation of cell states within a series string. |
| Thermal management | Control of heating and cooling to hold the pack in its safe and efficient window. |
| Communication and logging | Typically CAN in vehicles; the data source this project treats as its first-class transport. |

Design position taken by this project. The microcontroller is a monitor and is never the protection device. If the firmware hangs, crashes or is mid-reflash, the cell must still be safe. Every hardware configuration in Part IV places a protection circuit in series with the cell, independent of software.

## 4. State of Health, and Why It Is Hard

### 4.1 Definitions

State of health has no single definition. Two are in common use and they do not agree with each other:

- Capacity-based. SOH = present usable capacity divided by rated capacity. The definition used throughout this report.

- Resistance- or power-based. SOH expressed through internal-resistance growth relative to a new cell. Relevant where power delivery, rather than range, is the binding constraint.

A cell can be healthy on one definition and degraded on the other. Any claim about SOH estimation should therefore state which definition it is estimating, and this report states capacity throughout.

### 4.2 Why capacity is hard to measure in service

Four difficulties compound, and the first is the one this project ended up contributing to:

- There is no sensor for it. Capacity is not measured; it is inferred. A direct measurement requires a full controlled discharge between defined limits at a defined rate and temperature — which normal operation does not provide, and which a laboratory provides only at intervals.

- The measurement is condition-dependent. Measured capacity at a fixed cutoff depends on temperature and on discharge rate, because both affect the voltage drop that terminates the discharge. Two measurements of the same undegraded cell at different temperatures differ. Section 13 quantifies this for the data used here.

- The signal is slow and the noise is not. Fade over one cycle is far smaller than the repeatability of a capacity measurement, so a per-cycle fade label is dominated by noise. Section 11 measures exactly this and finds the target used in the original project design carries a maximum attainable R² of 0.044.

- Validation leaks. Because cycles from one cell are highly autocorrelated, a random train/test split over pooled cycles places near-duplicate rows on both sides. Reported skill under such splitting substantially overstates what the method would achieve on an unseen cell, and overstates it again for an unseen operating protocol. Part III is largely an account of how much.

### 4.3 The validation ladder

Prior work forms a ladder in which each rung holds out a larger unit than the last, and each exposes inflation the rung below concealed. This framing, and the two findings in its right-hand column, are taken from the literature verified in this project’s reference list.

| Rung | Holds out | Representative finding |
| --- | --- | --- |
| Random / k-fold over cycles | Nothing — cycles from one cell fall on both sides | Maher & Yerken (2025): R² = 0.9999 under random splitting |
| Cell-wise (LOBO) | One cell | Maher & Yerken (2025): the same data gives R² ≈ 0.91, described as optimistic bias |
|  |  | Le & Nguyen (2026): a 119% gap between 5-fold CV and LOBO on NASA |
| Protocol-wise (LOCO) | An entire operating protocol | Rare in the literature. The contribution of this project. |

Maher and Yerken (2025) is the closest prior work. They show that pooling cycles within a cell inflates skill and recommend group-wise cross-validation as the remedy. This project takes their conclusion as its starting point and shows that pooling protocols within a cohort inflates it again — and, further, that the obvious correction is itself too noisy to rank methods with at these sample sizes. The two results are consecutive rather than competing.

# PART II

      The Project: What BEACON Is and What We Built

## 5. Aims and Positioning

### 5.1 The original premise

The project began from a plausible and widely held premise: that how a battery has been used — its thermal exposure, its charge and discharge rates, its depth-of-discharge distribution — should predict how fast it degrades, and that a monitoring system could therefore score a cell from behavioural aggregates rather than from laboratory characterisation.

The first implementation was a rule-based scoring layer with hand-picked weights and thresholds, entirely unvalidated against real degradation data. This report is substantially the account of what happened when it was validated.

### 5.2 Objectives and outcomes

| Objective | Outcome |
| --- | --- |
| O1 — Ingest telemetry from heterogeneous transports onto one schema | Met. CAN, USB serial and dataset replay converge on one schema and one pipeline. |
| O2 — Derive behavioural features from usage telemetry | Met. C-rate, depth of discharge, thermal exposure and cycle segmentation implemented and tested. |
| O3 — Serve results through an API and dashboard | Met. FastAPI service, Express gateway, React client. |
| O4 — Demonstrate that behavioural scores predict capacity fade | Not met, and the reason is the project’s main result. See Part III. |
| O5 — Validate the ingest path on physical hardware | Met for voltage and current; temperature channel absent. See Part IV. |

On O4. A project reporting O4 as met would have had to ignore the evidence in Sections 11 and 14. This report treats not meeting it as the finding. What replaced it — that the standard validation protocol in this field cannot support the claims routinely made on it at these sample sizes — does not depend on batteries and is testable by anyone with two protocols and a held-out group.

## 6. System Architecture

Python (FastAPI, pandas, scikit-learn), Node (Express), React (Vite) and C++ firmware. Approximately 27,500 lines across 33 test modules with a seven-job continuous-integration pipeline.

### 6.1 Data flow

CAN bus  ─┐

USB rig  ─┼─► schema ─► features ─► coverage gate ─► scoring ─► API ─► dashboard

datasets ─┘

The coverage gate sits between the feature layer and scoring. Everything that reaches the dashboard has passed it, or arrives as a refusal carrying its reason.

### 6.2 Refusals as return values

Refusals are returned inside the result object rather than raised as exceptions. An exception would become an HTTP 500 and lose the reason; a refusal travels through the pipeline and reaches the interface intact, where it is rendered in place of the value it replaces. The governing rule, recorded as Architecture Decision Record 0004:

Any metric the input data cannot support is rendered as unavailable, with its reason, and is never replaced by a substituted or default value.

The practical consequence for anyone maintaining the system: a refusal in the output is not a defect. Making a number appear where the system has declined to produce one would defeat its purpose.

### 6.3 Decision records and evidence pinning

Fourteen Architecture Decision Records under docs/adr/ record each significant decision and what forced it. Separately, tests/test_reported_numbers.py pins every figure quoted in the documentation to the artefact it came from, with two assertions per claim: that the number is still present in the prose, and that the artefact still yields it.

This exists because figures went stale silently during development. The SOH ceiling moved from 0.612 to 0.569 when one cell left the screening criteria, and the NASA benchmark table was superseded twice; each was caught only by a human noticing. Derived figures are recomputed inside the test from recorded recipes rather than read from a stored column, so a changed recipe fails with the recipe stated.

## 7. Datasets and Experimental Frame

| Dataset | Cells | Cohort axis | Role |
| --- | --- | --- | --- |
| NASA Li-ion cycling (Saha & Goebel, 2007) | 34 (33 after screening) | Ambient temperature, 9 protocols | Primary calibration and validation |
| CALCE CS2 / CX2 prismatic series | 19–22 depending on derivation | Depth of discharge, 8–10 cohorts, 2 cell families | Independent replication |

A cohort is a group of cells sharing an operating protocol. The cohort axis differs deliberately between the two datasets: reproducing a result on the same axis would establish only that the analysis is repeatable, whereas reproducing it on a different axis establishes that the effect is a property of protocol shift rather than of temperature specifically.

## 8. Feature Layer and Scoring

Behavioural features are computed per cycle after segmentation into charge, discharge and rest phases. The segmentation thresholds are explicit and, being properties of the instrumentation rather than of the physics, are exposed as parameters:

| Constant | Value | Meaning |
| --- | --- | --- |
| REST_THRESHOLD_A | 0.5 A | Below this magnitude current is treated as rest, not charge or discharge |
| MIN_PHASE_SAMPLES | 3 | Consecutive samples past threshold before a phase change is accepted |
| COMPLETE_CYCLE_FRACTION | 0.80 | A discharge must move this fraction of the largest observed for that cell to count as complete |

Derived features include C-rate (current divided by declared rated capacity), aggressive-discharge and fast-charge flags defined by C-rate thresholds, deep-discharge flags from state of charge, and rolling thermal statistics. The rated capacity used as the C-rate denominator is declared by the measuring device rather than assumed by the host; if it is not supplied, scoring refuses rather than defaulting, because a wrong denominator silently rescales every behavioural feature.

# PART III

      What We Found

This part reports the calibration results. They are, in summary, negative for the project’s original premise and positive for a methodological question the project did not set out to answer.

## 9. Summary of Findings

- The original heuristic health index shows no statistically significant relationship with measured capacity fade: Spearman ρ = −0.269, p = 0.124, n = 33.

- Temperature exposure shows a real, cohort-controlled, statistically significant relationship with fade — but does not transfer across ambient conditions, for a measurement reason given in Section 13.

- The original prediction target, per-cycle capacity delta, has a signal fraction of 0.044. No method could have exceeded that R² against it.

- Leave-one-battery-out rank carries essentially no information about leave-one-cohort-out rank (ρ = +0.084, p = 0.795, n = 12).

- Across twelve methods, a straight line on cycle count is the most robust under protocol shift; all behavioural and nonlinear modelling buys approximately 0.05 R² over it.

- The leave-one-cohort-out estimator is approximately 2.7 times noisier than the effect it is used to rank. Six ranking claims were made and all six were withdrawn.

- 61% of the mean rule-based risk score comes from terms that are constant across the entire calibration set.

## 10. The Original Heuristic

The v1 health index was evaluated by ranking the 33 screened NASA cells by measured fade rate and correlating against the index. The result was ρ = −0.269 at p = 0.124 — not significant, and of the wrong sign. The index also produced only 6 distinct values across 33 cells, so most cells were indistinguishable to it.

Section 15 explains mechanically why: the majority of the score came from terms whose thresholds the data never crossed.

## 11. The Target-Definition Problem

This section should be read before interpreting any other result here. It determines what the other numbers mean.

### 11.1 Method

Each candidate target’s within-cell variance is decomposed into monotone trend and residual using isotonic regression against cycle index. A monotone fit assumes only that degradation does not reverse — the weakest assumption that still defines a trend — and was chosen over a polynomial, which would bend to absorb noise and overstate the recoverable signal. The trend fraction is a ceiling on attainable R², since nothing can predict the residual.

### 11.2 Results

| Target | Signal fraction (max attainable R²) | Cells | Rows |
| --- | --- | --- | --- |
| capacity_loss | 0.044 | 33 | 2,680 |
| soh / cumulative_fade | 0.569 | 31 | 2,585 |
| horizon_fade_10 | 0.389 | 31 | 2,268 |
| horizon_fade_20 | 0.639 | 25 | 1,933 |
| horizon_fade_50 | 0.967 | 17 | 1,246 |

An R² of 0.044 was the best score obtainable on the target against which this project’s central negative result was originally measured. Roughly 96% of that target is measurement noise.

### 11.3 Mechanism

The mechanism is arithmetic. A per-cycle capacity delta is the difference of two noisy measurements: it inherits both error terms while cancelling almost all of the underlying trend. The empirical distribution confirms it — mean 0.003 Ah, standard deviation 0.132 Ah, minimum −2.61 Ah. A cell does not recover 2.61 Ah in a single cycle; that value is noise, and it is in the labels.

### 11.4 Consequence

The original negative result — that no method beat a constant predictor — was real. Its scope was wrong.

- Defensible: these scores do not predict per-cycle capacity delta, which is mostly measurement noise.

- Not defensible: these scores do not predict degradation.

Against the cleaner soh target (ceiling 0.569) four candidate methods clear the bar the original target rejected. The methods were never as uninformative as the first framing suggested; the target was unsuitable.

## 12. Validation: LOBO versus LOCO

- LOBO — leave-one-battery-out. One cell held out; its protocol remains represented in training.

- LOCO — leave-one-cohort-out. An entire operating protocol held out. Substantially harder, and rare in the applied literature.

### 12.1 The collapse

Ranking 33 cells by measured fade rate, Spearman ρ, permutation-tested with 5,000 resamples:

| Candidate | ρ | p | Distinct outputs |
| --- | --- | --- | --- |
| v1 rule-based health index | −0.269 | 0.124 | 6 of 33 |
| v2 fitted OLS, in-sample | 0.870 | 0.0002 | 33 |
| v2, LOBO-refit (unseen cell, known protocol) | 0.841 | 0.0002 | 33 |
| v2, LOCO-refit (unseen protocol) | −0.295 | 0.097 | 33 |

The in-sample row is inadmissible and shown only to make the gap visible: the shipped v2 coefficients include a fitted intercept per cohort estimated on these same cells, and fade rate varies strongly by cohort. Refitting inside each fold is what makes the remaining rows meaningful.

ρ = 0.841 becomes ρ = −0.295 when the held-out axis changes from cell to protocol. Same model, same data, same features.

### 12.2 Selecting on LOBO selects the wrong model

Twelve published methods, including a genuine XGBoost and a genuine LSTM over ten consecutive cycles per cell, were evaluated under both protocols. LOBO rank carries essentially no information about LOCO rank: ρ = +0.084, p = 0.795, n = 12. Selecting a method by LOBO costs 0.309 R² relative to selecting by LOCO.

## 13. Benchmark Results

Target soh, 2,585 rows, 31 cells, 9 cohorts, ceiling 0.569. Sorted by LOCO R².

| Method | LOBO MAE | LOCO MAE | LOBO R² | LOCO R² | Δ |
| --- | --- | --- | --- | --- | --- |
| xgboost | 4.21% | 7.62% | 0.732 | 0.459 | −0.273 |
| age_linear | 8.54% | 10.71% | 0.483 | 0.406 | −0.076 |
| elasticnet | 7.61% | 10.31% | 0.609 | 0.355 | −0.254 |
| gpr_matern | 4.48% | 17.06% | 0.725 | 0.207 | −0.518 |
| random_forest | 4.90% | 10.67% | 0.773 | 0.150 | −0.623 |
| svr_rbf | 6.91% | 14.29% | 0.651 | 0.087 | −0.564 |
| age_quadratic | 6.62% | 8.31% | 0.336 | 0.034 | −0.301 |
| age_isotonic | 6.99% | 8.50% | 0.278 | 0.018 | −0.260 |
| train_mean | 11.17% | 11.92% | 0.000 | 0.000 | 0.000 |
| lstm | 5.62% | 17.36% | 0.594 | −0.185 | −0.778 |
| hist_gradient_boosting | 4.12% | 10.27% | 0.770 | −0.265 | −1.035 |
| mlp | 4.15% | 14.19% | 0.731 | −0.623 | −1.354 |

- Every method loses skill under protocol shift. The question is only how much.

- The most robust is age_linear, a straight line on cycle count, with Δ = −0.076. It reaches LOCO R² = 0.406 against the best model’s 0.459.

- All behavioural and nonlinear modelling therefore buys approximately 0.05 R² over counting cycles.

- The three best LOBO performers — random_forest (0.773), hist_gradient_boosting (0.770), mlp (0.731) — rank 5th, 11th and 12th under LOCO, and two score below a constant predictor.

The neural results deserve comment given how often such architectures are reported as successful on this dataset. Both the LSTM and the MLP achieve competitive LOBO scores and both fall below a constant predictor under protocol shift, which is consistent with learning cohort-specific intercept structure rather than a transferable degradation relationship.

## 14. The Reversible Thermal Offset

Section 12 established the cross-cohort collapse statistically. This section gives it a measurement explanation, and it is the point in this report where the electrochemistry of Part I becomes load-bearing.

### 14.1 Observation

Apparent state of health measured at cycle index ≤ 20 — before meaningful degradation is possible — varies systematically with ambient temperature:

| Ambient | Apparent SOH at cycle ≤ 20 |
| --- | --- |
| 4 °C | 0.918 |
| 44 °C | 0.999 |

An eight-point spread in apparent SOH exists before any cell has aged. This is the resistance-rise row of Section 2.3 acting through temperature rather than through degradation: at low temperature, elevated impedance and slower kinetics curtail the discharge at the cutoff voltage, so less capacity is extracted from an undegraded cell. It is a reversible offset in the measurement, not a loss of lithium inventory or active material.

### 14.2 Why it inverts the cross-cohort relationship

Within a fixed-ambient cohort the offset is a constant. It shifts the intercept and leaves the within-cohort temperature-versus-fade relationship intact — and that relationship is real, cohort-controlled and statistically significant.

Across cohorts the offset switches on, and it is anti-correlated with genuine thermal ageing: hot cells show higher apparent capacity from the offset while degrading faster in truth. The two effects oppose, the offset dominates at low cycle counts, and the apparent sign of the relationship reverses.

Consequence for the feature layer. The current-based signals avg_stress and aggressive_discharge_count are significant and positive in room-temperature cohorts, and significant and negative in cold cohorts. A model fitted across cohorts without accounting for the offset is fitting a sign change.

This is a strong argument for normalising measured capacity to a controlled reference temperature before any cross-protocol comparison. This project does not perform that step, and Section 20 lists it as the single most valuable piece of future work.

## 15. Estimator Variance and Withdrawn Claims

Five ranking claims had been made and withdrawn by the midpoint of this work. Rather than make a sixth, a designed experiment of 220 measurements was run to establish why they kept failing to replicate.

### 15.1 The coverage hypothesis, refuted

The proposed explanation was that the LOBO-to-LOCO gap reflects cohort coverage, and that more cohorts in training would close it. It was refuted: the one dataset showing a significant raw correlation lost it entirely once training-set size was regressed out. On the replication, raw ρ(cohorts, gap) = +0.126, p = 0.217, n = 98.

### 15.2 What the experiment established

The LOCO estimate has an interquartile range across cohort draws of 0.724 R², against a median difference between a nonlinear model and a straight line on cycle count of 0.351 R².

The measurement is roughly twice as noisy as the effect it is being used to rank. Every ranking claim failed to replicate because the instrument could not resolve the quantity.

### 15.3 Self-correction against a corrected target

That result was itself re-examined against a corrected target derivation — same cells, features, methods and machinery, differing only in target derivation, restricted to the three coverage levels both runs draw fully (k = 3, 4, 5).

| Quantity | Cycle_Index target | Full-discharge target |
| --- | --- | --- |
| LOCO IQR of the gap | 0.892 | 0.296 |
| Median paired svr_rbf − age_linear | −0.336 | −0.110 |
| Draws where svr_rbf wins | 13.9% | 38.9% |
| Noise-to-effect ratio | 2.66 | 2.70 |

The IQR reduction is 0.596 R², bootstrap 95% confidence interval [0.335, 0.936] over 4,000 resamples; the corrected estimate is smaller in every resample. Three distinct conclusions follow:

- The claim survives as a ratio. 2.70 against 2.66 — the estimator is several times noisier than the effect on both derivations. Not an artefact of the target.

- The magnitudes were inflated roughly threefold. Quoting 0.724 or 0.351 as a property of leave-one-cohort-out in general overstates it by that factor; those figures describe that estimator on that frame.

- The mechanism does not survive. On the Cycle_Index target svr_rbf collapsed hardest; on the corrected target the ordering inverts. “The flexible method transfers worst” is the sixth withdrawn ranking claim.

### 15.4 Standing position

At the sample sizes standard battery datasets provide, a single leave-one-cohort-out estimate cannot distinguish between candidate methods and must be reported as an interval.

This is a methodological contribution independent of which model wins, and it is the result this project would offer for publication.

## 16. Threshold Reachability of the Risk Score

A separate audit asked whether the rule-based risk score’s hand-chosen cut points are reachable by real data. Of a mean risk score of 52.3 points, 32.0 points — 61% — come from terms that are constant across the entire NASA fleet, because their thresholds sit outside the range the data occupies.

This explains mechanically why the heuristic showed no resolution between cells, and reframes the earlier null result as a calibration-design fault rather than a failure of the behavioural premise itself. It is the most recoverable of the negative findings: the premise may yet hold under thresholds chosen from data rather than by hand.

# PART IV

      Hardware: What We Are Doing Now

Parts I to III are dataset work. This part documents the physical bench rig built to close the loop from instrument to dashboard, and is reported with a strict separation between what has been measured and what has not.

## 17. Rig Design and Component Rationale

| Function | Selected | Rejected alternative and reason |
| --- | --- | --- |
| Current and bus voltage | INA219, I²C, 0.1 Ω 2 W shunt, high-side | ACS712 — analogue output inherits ADC nonlinearity, and its zero-current offset drifts with temperature, which is fatal for coulomb counting. |
| Terminal voltage | INA219 bus channel | Resistive divider to ADC — adds 1.4% resistor-tolerance error, drains the cell continuously, and the ESP8266 ADC is nonlinear near the rails. |
| Temperature | LM35DZ fitted; DS18B20 preferred | NTC thermistor — a disconnected NTC floats to a plausible in-range value and is scored as a measurement. A disconnected DS18B20 reports −127 °C and is rejected by the schema. |
| Protection | Protected cell plus TP4056/DW01 module | None — the microcontroller is a monitor and must never be the protection device. |
| Controller | ESP8266 NodeMCU | ESP32 not required: with the INA219 on I²C, no analogue channel is needed for voltage or current. |

The temperature criterion is worth stating explicitly, because it is a systems argument rather than a component one: the part whose failure mode is detectable was preferred over the part with better nominal accuracy. The schema declares temperature valid over −40 to 150 °C, so a sensor whose failure produces a value inside that range is indistinguishable from a working one.

### 17.1 Shunt sizing and error budget

The INA219 shunt channel is ±320 mV full scale at 12 bits. With a 0.1 Ω shunt this gives 3.2 A full scale and a 100 µA least significant bit. Discharge must stay below 3.2 A; saturation is not a graceful failure, since a clipped reading is silently wrong rather than flagged. At 2 A the shunt dissipates 0.4 W, and its temperature coefficient makes a hot shunt read high, which makes current read low — a systematic capacity error in one direction.

## 18. The Wire Protocol

The firmware-to-host contract is beacon.telemetry.v1. Every line carries the sentinel BEACON1, a record type, a body, and an optional NMEA-style XOR checksum appended as *HH:

BEACON1 D {"t":0.138,"v":3.9880,"i":0.0000,"soc":100.00}*0F

- Checksum optional, enforced when present. A checksum verified only sometimes is worse than none, so a line carrying *HH must verify or the record is refused.

- Sentinel resync. The parser searches for the sentinel anywhere in the line rather than at position zero. Added after a real capture failure: a post-reset board emits boot output, so the HELLO line arrived concatenated with reset noise and was discarded.

- Capacity declared, not assumed. HELLO carries capacity_ah, bounded to 0.01–500 Ah. If neither rig nor caller supplies it, scoring refuses rather than defaulting.

- Sensor complement declared. The rig probes its sensors at startup and declares only the channels it can supply. A channel that disappears mid-capture is then a detectable fault rather than a silent gap.

## 19. Measured Results

### 19.1 Cell under test

| Property | Value |
| --- | --- |
| Cell | HONGLI ICR-18650-2200mAh, protected |
| Chemistry | ICR (LiCoO₂) — see Section 1.2 |
| Nominal voltage | 3.7 V |
| Rated capacity | 2200 mAh (2.2 Ah), declared on the wire, not independently verified |
| Energy | 8.14 Wh |

### 19.2 Capture

83 accepted data records over 82.2 s at 1 Hz, cell at rest with no load connected:

| Channel | Mean | Minimum | Maximum | n | Status |
| --- | --- | --- | --- | --- | --- |
| Terminal voltage | 3.9871 V | 3.9840 V | 3.9920 V | 83 | Measured |
| Current, signed | −0.0000 A | −0.0004 A | 0.0004 A | 83 | Measured |
| Cell temperature | — | — | — | 0 | Not supplied |

#### Instrument characterisation

- Every voltage reading is an exact multiple of 4 mV, the INA219 bus-channel least significant bit. The converter resolves at its native resolution with no observable drift across the capture.

- The current channel noise floor at zero current is ±0.4 mA over n = 83, with 48 of 83 samples reading exactly zero. A measured instrument characteristic, not a datasheet figure.

- Frame acceptance 83/83 (100%), zero checksum failures, zero non-conforming lines.

### 19.3 The refusal, in service

With temperature absent, the coverage gate declined to score:

signal coverage: INCOMPLETE

missing: temperature_c

MISSING temperature_c -> needed by behaviour features

(high_temp_flag, temp_rolling_*)

This rig cannot drive the full feature pipeline.

The pipeline accepted every record, compared delivered channels against those the feature layer requires, and declined to score — naming the missing channel and the features that depend on it. The voltage and current measurements are unaffected and are reported alongside the refusal, on the dashboard as well as in the log.

### 19.4 What the hardware does not establish

Stage A — transport validated. An earlier capture of 151/151 accepted records validated framing, checksums, sentinel resync and time monotonicity on physical silicon. That firmware ran synthetic sensor stubs: the numbers were generated on the board and carried over a real wire. It validates the transport, not any measurement. Stage B — measurement, partially. Voltage and current are genuine instrument readings from a physical cell. Temperature is absent; the rig declined to declare the channel and the gate consequently refused to produce health, RUL or SOH. Not established. No coulomb-counting accuracy claim, because no independent reference instrument was available. No charge-side behaviour recorded. No capacity measurement performed.

### 19.5 Integration constraint encountered

The CH340 USB-to-serial bridge on the development board accepts only 9600 and 19200 baud; 38400 and above are refused at the driver level. This was diagnosed by probing the baud ladder rather than assumed. The firmware’s serial rate is a build-time override, so the board-specific value was applied without changing the repository default of 115200, which would otherwise have desynchronised firmware and host for every other user.

# PART V

      Where We Are and What We Will Do

## 20. Current Status

| Area | State |
| --- | --- |
| Ingest and schema | Complete. Three transports, one schema, one pipeline. |
| Feature layer | Complete and tested; temperature-dependent features unexercised on hardware. |
| Calibration and validation | Complete. Findings in Part III; six ranking claims withdrawn. |
| API and dashboard | Complete. Measured hardware values shown separately from simulated fleet values. |
| Hardware — transport | Validated. 151/151 records accepted on physical silicon. |
| Hardware — voltage and current | Measured on a real cell. 83/83 records accepted. |
| Hardware — temperature | Not functional. Channel undeclared; gate refuses to score. |
| Hardware — capacity accuracy | Not attempted. No reference instrument. |
| Literature survey | Incomplete. Left in that state rather than padded. |

## 21. Limitations and Threats to Validity

### 21.1 Statistical

- Sample size. 33 cells across 9 cohorts is small for cohort-level inference. The estimator-variance result of Section 15 is precisely a statement about this limitation, and applies to this project’s own conclusions as much as to anyone else’s.

- Cohort imbalance. Three to four batteries per cohort is insufficient to identify a mixed-effects variance component, which is why a full LOBO cross-validation of the mixed model was deliberately not run: with an unidentified variance component the number would not have been interpretable.

- Single-frame estimates. Any figure from one LOCO draw should be read as an interval, not a point. This is why no ranking claim is offered.

### 21.2 Measurement

- The reversible thermal offset of Section 14 is not corrected for. Cross-cohort results should be read with that confound present.

- Capacity is taken from each dataset’s reported discharge capacity and inherits whatever protocol that laboratory used.

### 21.3 Hardware

- No independent reference instrument, so coulomb-counting accuracy is unvalidated and no accuracy claim is made.

- Temperature channel not functional; all temperature-dependent behavioural features unexercised on hardware.

- Measurements at rest only. No discharge above the 0.5 A rest threshold, so cycle segmentation is unexercised on live hardware.

- Single cell, single rig, single capture. No repeatability statistics across cells or sessions.

### 21.4 Scope

- The literature survey is incomplete and is left in that state rather than padded.

- Committed conformal-prediction artefacts did not reproduce exactly on re-run, with a fold-count discrepancy. Recorded as open; the pinned figures were not adjusted to match the new run.

## 22. What We Will Do Next

### 22.1 Immediate — completing the hardware loop

- Restore the temperature channel. Substitute a DS18B20 for the LM35, recovering a sensor whose failure mode is detectable by the schema without a firmware plausibility floor. Unblocks the coverage gate and the temperature-dependent features.

- Add a resistive load and record a discharge. A 3.3–4.7 Ω power resistor draws 0.8–1.1 A at 3.7 V, above the 0.5 A rest threshold, exercising phase segmentation and C-rate on live hardware for the first time.

- Record a charge cycle through the TP4056. Completes the cycle and exercises fast_charge_flag and the charge-side behaviour features, none of which has ever seen hardware data.

### 22.2 Near term — making a measurement claim

- Acquire an independent capacity reference. An 18650 analyser with discharge-capacity readout permits a coulomb-counting accuracy statement. Without it the rig can only be shown to agree with itself, which is not a result.

- Cross-validate the instrument. Compare INA219 bus voltage against a multimeter, and INA219 current against the Ohm’s-law prediction from a measured load resistance. Two independent checks requiring no additional instrument beyond a meter.

### 22.3 Research — the findings that matter

- Capacity normalisation to a reference temperature. Section 14 identifies the reversible thermal offset as the largest confound in the cross-cohort analysis. Normalising measured capacity before comparison is the single highest-value scientific step available.

- A dataset with 8–10 or more cells per cohort. Sufficient to identify the mixed-effects variance component the present data cannot, closing the modelling line left open in Section 21.1.

- Re-derive the risk thresholds from data. Section 16 shows 61% of the score comes from unreachable terms. Thresholds chosen from the observed distribution rather than by hand would test the behavioural premise properly for the first time.

- Interval reporting as standard. Adopt Section 15.4 as policy: every leave-one-cohort-out estimate reported as an interval across cohort draws, never as a point.

### 22.4 Publication

The methodological result of Section 15.4 is the publishable contribution. It is dataset-independent, it has replicated across two laboratories and two cohort axes, and it is testable by anyone with two protocols and a held-out group. The intended framing is a short methods paper reporting that leave-one-cohort-out estimates at standard battery-dataset sample sizes cannot rank candidate methods, with the six withdrawn claims as the evidential record.

## 23. Conclusions

- The prediction target originally chosen, per-cycle capacity delta, is approximately 96% measurement noise, with a maximum attainable R² of 0.044. Target definition dominated the original negative result.

- Model ranking under leave-one-battery-out validation carries essentially no information about ranking under leave-one-cohort-out validation (ρ = +0.084, p = 0.795, n = 12), and selecting on the former costs 0.309 R².

- Across twelve published methods, a straight line on cycle count is the most robust under protocol shift; all behavioural and nonlinear modelling buys approximately 0.05 R² over it.

- A reversible thermal offset of approximately 8 SOH points exists in apparent capacity before any degradation, is constant within a cohort and anti-correlated with true thermal ageing across cohorts, and mechanically explains the sign reversal in cross-cohort fitting.

- At these sample sizes a single leave-one-cohort-out estimate is roughly 2.7 times noisier than the effect it is used to rank. Six ranking claims were made and all six withdrawn.

- 61% of the rule-based risk score is constant across the calibration set, reframing the original null as a calibration-design fault rather than a refutation of the behavioural premise.

- A physical rig measures terminal voltage and current on a real cell, and the validation gate correctly refuses to produce health, RUL or SOH when a required channel is absent.

Closing position. The project did not demonstrate that behavioural scores predict capacity fade. It demonstrated why the question is harder to answer than the literature’s validation practice suggests, and it built a system that declines to answer it rather than answering it badly. The refusals are the engineering deliverable.

# PART VI

      Appendices

## Appendix A: Reproduction

Every command below runs on a fresh clone with no hardware, no database, no API keys and no dataset download.

git clone https://github.com/Navvu-gityhub/Behavior-Aware-BMS.git

cd Behavior-Aware-BMS

pip install -r requirements-dev.txt

python main.py                      # end-to-end run

python scripts/run_serial_demo.py   # rig -> parser -> gate

python -m pytest tests/ -q          # 33 test modules

Replay of the hardware capture reported in Section 19.2:

python scripts/run_serial_demo.py --replay \\

data/interim/rig_stage_b_voltage_verified.txt

Firmware build for the bench rig, with board-specific serial rate and real sensors:

arduino-cli compile --fqbn esp8266:esp8266:nodemcuv2 \\

--build-property "compiler.cpp.extra_flags=\\

-DSERIAL_BAUD=9600 -DUSE_REAL_SENSORS=1" \\

firmware/beacon_rig

## Appendix B: Glossary

| Term | Meaning |
| --- | --- |
| C-rate | Current divided by rated capacity. 1 C discharges a cell in one hour. |
| Cohort | A group of cells sharing an operating protocol (a temperature, a depth of discharge). |
| Coulomb counting | Integrating current over time to track charge moved. |
| DOD | Depth of discharge — the fraction of capacity removed in a discharge. |
| Knee point | The cycle at which near-linear capacity fade begins to accelerate. |
| LAM | Loss of active material — electrode material no longer electrochemically accessible. |
| LLI | Loss of lithium inventory — cyclable lithium consumed by side reactions. |
| LOBO | Leave-one-battery-out validation. Holds out one cell. |
| LOCO | Leave-one-cohort-out validation. Holds out an entire operating protocol. |
| OCV | Open-circuit voltage — terminal voltage at rest, with no current flowing. |
| RUL | Remaining useful life, in cycles. |
| SEI | Solid-electrolyte interphase — the passivating film on the negative electrode. |
| Signal fraction | Share of a target’s variance that is monotone trend; a ceiling on attainable R². |
| SOC | State of charge — present charge as a percentage of present capacity. |
| SOH | State of health — here, present capacity as a fraction of rated capacity. |

## Appendix C: References

Every entry below was verified against the publisher’s or repository’s own record in the source project. No reference here was filled in from memory. The literature survey as a whole remains incomplete, and is reported as such in Section 21.4 rather than padded.

- B. Saha and K. Goebel (2007). “Battery Data Set”, NASA Prognostics Data Repository, NASA Ames Research Center, Moffett Field, CA. Primary calibration dataset: 34 Li-ion cells, 7.24M telemetry rows, measured per-cycle discharge capacity across 9 documented protocols.

- CALCE Battery Research Group, University of Maryland. PL pouch cell calendar-ageing and capacity-characterisation data. Found unsuitable for the calibration questions attempted, for reasons specific to the files supplied.

- K. A. Severson, P. M. Attia, N. Jin, N. Perkins, B. Jiang, Z. Yang, M. H. Chen, M. Aykol, P. K. Herring, D. Fraggedakis, M. Z. Bazant, S. J. Harris, W. C. Chueh and R. D. Braatz (2019). “Data-driven prediction of battery cycle life before capacity degradation”, Nature Energy, 4(5), 383–391. doi:10.1038/s41560-019-0356-8

- K. Maher and N. Yerken (2025). “Comprehensive machine learning for lithium-ion battery state-of-health estimation using group-wise cross-validation”, 14th International Conference on Renewable Energy Research and Applications (ICRERA 2025), pp. 1465–1468, IEEE. doi:10.1109/ICRERA66237.2025.11283788. The closest prior work to this project’s methodological contribution.

- H. H. Le and K.-A. Nguyen (2026). “Charging phase health indicators for battery state-of-health estimation: a systematic comparison of CC, CV, and combined approaches under cross-battery validation”, arXiv:2607.23482. Cited from the abstract; the 119% figure should be confirmed against the full text before being quoted elsewhere.

- Y. Liu, S. Saxena, M. Pecht et al. CALCE CS2 and CX2 prismatic cell cycling series, Center for Advanced Life Cycle Engineering, University of Maryland. Replication dataset: 22 cells across 10 cohorts under the corrected full-discharge derivation, spanning two cell families and a depth-of-discharge cohort axis.

## Appendix D: Key Artefacts in the Repository

| Path | Contents |
| --- | --- |
| docs/final_report.md | Full analysis, every section referenced above |
| docs/adr/ | Fourteen architecture decision records |
| docs/hardware_design.md | Sensor selection, shunt sizing, error budget, safety |
| docs/protocol_design.md | beacon.telemetry.v1 wire format |
| tests/test_reported_numbers.py | Prose-to-evidence pinning for every quoted figure |
| reports/metrics/ | Tracked result artefacts; live test inputs |
| firmware/beacon_rig/ | Rig firmware; USE_REAL_SENSORS selects sensors or synthetic profile |
| data/interim/rig_stage_b_voltage_verified.txt | The hardware capture reported in Section 19.2 |